Magnetic spin dynamics in Mn-hureaulite

SoHyun PARK1 and Ana Arauzo2

1Department of Geo- and Environmental Sciences, Section of Crystallography, 
Ludwig-Maximilians-Universität München, 80333 Munich, Germany; 2Instituto de Nanociencia y Materiales de Aragón, CSIC-Universidad de Zaragoza and Departamento de Física de la Materia Condensada, 50009 Zaragoza, Spain.

A hureaulite-type synthetic compound, Mn2+5(PO4)2(PO3(OH))2(HOH)4 undergoes complex magnetic phase transitions. At 6.17 K, the paramagnetic (PM) phase (space group: C2/c) transforms to inherit a ferrimagnetic (FM) order (magnetic space group: C2’/c’), followed at 1.86 K by an incommensurately modulated antiferromagnetic (AFM) order (magnetic superspace group: P21/c.1’((0()00s with the propagation vector k(0.523(2), 0, 0.055(1)) [1]. In the FM state, AFM interactions are dominant for both intra and inter pentamers of Mn2+(O, HOH)6 octahedra. Differently aligned spin-canting sublattices at three unique Mn sites in the FM phase explains a weak ferromagnetism in the title compound. More interestingly, magnetic spin-canting reorientations continuously proceed below the Curie temperature (Tc = 6.17 K), e.g. at 6.1 K, all three Mn sites exhibit large values for magnetic moments in a direction, but at 3.4 K in c direction (Fig. 1).

This vivid spin dynamic system could be confirmed by alternating current magnetic susceptibility ((ac) at Hac = 5 Oe within a frequency (f) window of 10-10000 Hz. In Fig. 2, the acquired (ac spectra demonstrate high and complex dynamics in the whole temperatures (T) covering all PM/FM/AFM regions. The presence of the out-of-phase part (’’ac  > 0 below Tc agrees with a strong (T, f)-dependent reorientations of magnetic spins. Around Tc, as frequency increases, (’ac decreases, but (’’ac increases and shifts to higher temperatures. A minimum of in the real part ((’ac) at 5.28 K shifts to lower temperatures at elevated frequencies. Both (’ac and (’’ac below 2.6 K show two extremely different tendencies below and above 2500 Hz. More details of these vital magnetic spin dynamics are reported at the meeting DGK 2022.

[1] Park, S.-H. Hartl, A., Sheptyakov, D, Hoezel, M., Arauzo, A. Structural Investigation into Magnetic Spin Orders of a Manganese Phosphatic Oxyhydroxide, Mn5[(PO4)2(PO3(OH))2](HOH)4. Symmetry 2021, 13(9), 1688 (pp18).