Element replacement in Mo2Ga2C via molten salt synthesis

Catherine Schweinle1, Dr. Martin Ade1, Prof. Dr. Harald Hillebrecht1

1 Institute of Inorganic and Analytical Chemistry, Faculty of Chemistry and Pharmacy, Albert-Ludwigs-Universität Freiburg, Albert Str. 21, 79104 Freiburg im Breisgau, Germany

The molten salt synthesis of MAX-phases has been known for over ten years [1]. Using Lewis-acids like ZnCl2 or CuCl2 offers a way to synthesize MXenes without HF. The procedure is known for more than just titanium-based MAX-phases like Ti3AlC2. Using ZnCl2, the synthesis is limited to Al-containing MAX-phases [2]. By using Lewis-acids with a higher redox-potential, the method can be extended for other A elements like gallium or silicon [3]. Other metals like tantalus or niobium could also be delaminated. By molten salt synthesis, the A metal could also be replaced by the metal of the Lewis acid. Herein, we report the partial replacement of gallium by copper using Mo2Ga2C, CuCl and CuCl2.

The reaction between Mo2Ga2C and CuCl/CuCl2 ends in the formation of Mo2C according to 1.1

Mo2Ga2C + 3 CuCl2 → Mo2C + 3 Cu + 2 GaCl3					1.1

Adding RbCl allows for a lower reaction temperature, due to the formation of an eutectic system.

During variation of the reaction temperature, the formation of a new MAX-phase could be observed via XRD. EDX measurement identified this phase as Mo2Ga1-xCuxC, where x is 2/3. Excess copper could be easily removed by treating the sample with concentrated HCl under reflux.

Fig. 1 EDX mapping of Mo2Ga1-xCuxC

[1]	W.-B. Tian, P.-L. Wang, Y.-M. Kan et al., “Cr2AlC powders prepared by molten salt method,” J. Alloys Compd., vol. 461, 1-2, L5-L10, 2008.

[2]	M. Li, J. Lu, K. Luo et al., “Element Replacement Approach by Reaction with Lewis Acidic Molten Salts to Synthesize Nanolaminated MAX Phases and MXenes,” JACS, vol. 141, no. 11, pp. 4730–4737, 2019.

[3]	Y. Li, H. Shao, Z. Lin et al., “A general Lewis acidic etching route for preparing MXenes with enhanced electrochemical performance in non-aqueous electrolyte,” Nat. Mater., vol. 19, no. 8, pp. 894–899, 2020.