From binary to ternary amalgams: expanding the structural variety of the Gd14Ag51 structure family

Timotheus Hohl1, Lukas F. J. S. Nusser1, Jessica Wulfes2, Constantin Hoch1
1Department Chemistry and Biochemistry, Chair of Inorganic Solid State Chemistry, LMU Munich, Germany
2Institute of Physical Chemistry, Christian-Albrechts-University, Kiel, Germany
Mercury-rich amalgams serve as ideal candidates for the investigation of structure-property-relationships in polar intermetallic phases. These intermetallic compounds, which consist of very precise stochiometric constitutions, unite both ionic as well as metallic bonding shares, resulting in rather unusual properties, such as the so-called “bad-metal-behaviour”.
Fig 1: Unit cell of Yb10.5Sr0.5Hg54. Hg (gray), Polyhedra: Yb (pink), Yb0.86Ca0.14 (green).
Within this compound class, the Gd14Ag51 structure represents the aristotype of many binary mercury-rich amalgams [1]. Apart from Yb11Hg54, each binary amalgam of this type exhibits individual disorder phenomena – from mixed occupation, over mutually exclusive sets of atoms as well as enlarged translation vectors while still exhibiting common structural features and compositions. With each compound containing more than 100 atoms per unit cell, these structures possess a rather high level of structural complexity which can be compared with the aid of complexity measures [2].
Fig 2: Unit cell of Ca6.5Na4.5Hg54. Hg (gray), Polyhedra: Na0.84Ca0.16 (green), Na0.64Ca0.36 (blue), Na0.2Ca0.8 (yellow) Ca (pink).
Through the use of single-crystal and synchrotron X-ray diffraction, we have identified and characterised three new ternary amalgams and thereby increased the variety of the known compounds in this structure type. Surprisingly, these compounds still show the structural features of the Gd14Ag51 aristotype, but exhibit new disorder phenomena (cf. Fig. 1 - 3 ).
Fig. 3: Unit cell of Ca4.5Eu6.5Hg54. Hg (gray), Polyhedra: Eu0.9Ca0.1 (green), Eu0.78Ca0.22 (blue), Eu0.45Ca0.55 (orange), Eu0.33Ca0.67 (yellow), Hg underoccupation along 0, 0, z (red).
[1]	Tambornino F., Sappl J., Hoch C.; The Gd14Ag51 structure type and its relation to some complex amalgam structures. J. Alloys Compd., 618, 326–335 (2015)
[2]	Dshemuchadse J., Steurer W.; Some statistics on intermetallic compounds. Inorg. Chem.,54, 1120–1128 (2015)

We acknowledge support by DFG under project number 429690805.