Anisotropic magnetoresistance and Magnetic properties of epilayers-perovskite LBMTO

Marwene Oumezzine1, Aurelian Catalin Galca2, Victor Kuncser3

1Laboratoire de Physico-chimie des Matériaux, Université de Monastir, Monastir, Tunisia.

2Laboratory of Multifunctional Materials and Structures, National Institute of Materials Physics, Magurele, Romania

3Laboratory of Magnetism and Superconductivity, National Institute of Materials Physics, Magurele, Romania

An epitaxial thin film of (LBMTO) was synthesized using pulsed laser deposition technique (PLD) with a desirable thickness of 95 nm. The film grown on SrTiO3 (0 0 1) substrates exhibited a paramagnetic-to-ferromagnetic second order phase transition at 291 K. The as-grown film displays a giant magnetoresisitance (GMR) up to 150% at room temperature under 5T applied magnetic field.

A.K.A. acknowledges support by DFG under grant number Alph999/99-0.