## Slide 1
SANS: a powerful tool to probe foams and emulsions
Fabrice.cousin@cea.fr

## Slide 2
Outline…
Pickering emulsions based on cellulose nanocrystals
Foams and Neutron Scattering
Strategy 2 : Smart Foams based on fatty acids
Ultrastable and thermo-stimulable foams
Strategy 1 : Foams based on SDS and salt
Ultrastable and thermo-stimulable foams

## Slide 3
Outline…
Pickering emulsions based on cellulose nanocrystals
Foams and Neutron Scattering
Strategy 2 : Smart Foams based on fatty acids
Ultrastable and thermo-stimulable foams
Strategy 1 : Foams based on SDS and salt
Ultrastable and thermo-stimulable foams

## Slide 4
1 µm
Pickering emulsions
Use of Nanocrystals Cotton Cellulose (NCCs)
(« Pickering » emulsions)
F. Cherhal et al, Biomacromolecules, 2016, 17(2), pp 496–502
Design of emulsions by green bio-based compounds ?
What are the mechanisms of stabilization ?

## Slide 5
5
1
2
4
3
6
Cellulose
Glucose
5
1
2
4
3
6
Cellulose
Fibers
Hydrolysis of amorphous parts
SO3-
SO3-
SO3-
SO3-
Cotton
What are NCCs ?
Pickering emulsions

## Slide 6
5
1
2
4
3
6
Cellulose
Glucose
5
1
2
4
3
6
Cellulose
Fibers
What are NCCs ?
Charge density :
0.16 e/nm2
Possible Desulfatation
Charge density :
< 0.01 e/nm2 («neutral »)
After hydrolysis
Hydrolysis of amorphous parts
SO3-
SO3-
SO3-
SO3-
Cotton
Pickering emulsions

## Slide 7
What is the behavior of NCCs in solution ?
SANS
F. Cherhal et al, Langmuir, 2015, 31(20), 5596–5602
Pickering emulsions

## Slide 8
SANS
Fit by paralleliped form factor
(6nm x 22nm x 195nm)
Aggregation at high salinity (Df = 2.1 )
NaCl
Charge density : 0.16 e/nm2
Neutrons
What is the behavior of NCCs in solution ?
Pickering emulsions

## Slide 9
Neutrons
SANS
q-2.3
Aggregates whatever salinity
More compact than for charged NCCs
Charge density : < 0.01 e/nm2
What is the behavior of NCCs in solution ?
Pickering emulsions

## Slide 10
Low concentration : droplets diameter when mp
More interface is stabilized
(Neutral)
(Charged)
Water
Oil
% /
(Quantity of NCC/oil)
Two regimes :
High concentration : diameter ~ stable
?
?
Pickering emulsions

## Slide 11
(Neutral)
(Charged)
Water
Oil
% /
(Quantity of NCC/oil)
Two regimes :
?
?
Densification of interfacial layer ?
Multilayers formation ?
Excess of NCC in aqueous phase ?
Pickering emulsions

## Slide 12
3 different possible contrasts for neutrons
Neutrons
Neutrons
Neutrons
F. Cherhal et al, Biomacromolecules, 2016, 17(2), pp 496–502
Pickering emulsions

## Slide 13
At local scale : Infinite plane
F. Cherhal et al, Biomacromolecules, 2016, 17(2), pp 496–502
Pickering emulsions

## Slide 14
q-2
Direct Reading of thickness
At local scale : Infinite plane
F. Cherhal et al, Biomacromolecules, 2016, 17(2), pp 496–502
Pickering emulsions

## Slide 15
q-2
Direct Reading of thickness
At local scale : Infinite plane
Interface saturated below a given NC quantity
Rinsed
Not rinsed
F. Cherhal et al, Biomacromolecules, 2016, 17(2), pp 496–502
Pickering emulsions

## Slide 16
q-2
Direct Reading of thickness
Monolayer : breaking of aggregates previously formed in solution
(strong stirring to make emulsion)
Thickness : one NC !!
At local scale : Infinite plane
Densification rather than multilayers formation
F. Cherhal et al, Biomacromolecules, 2016, 17(2), pp 496–502
Pickering emulsions

## Slide 17
q-2
Aggregates at the interface
Thickness independent of the NCC quantity (??)
Direct Reading of thickness
At local scale : Infinite plane
F. Cherhal et al, Biomacromolecules, 2016, 17(2), pp 496–502
Pickering emulsions

## Slide 18
Q-4
Porod law :
Smooth interface
Deviation from Porod law :
Rough Interface
F. Cherhal et al, Biomacromolecules, 2016, 17(2), pp 496–502
Pickering emulsions

## Slide 19
Q-4
Porod law :
Smooth interface
Deviation from Porod law :
Rough Interface
NCC do not dive into oil
F. Cherhal et al, Biomacromolecules, 2016, 17(2), pp 496–502
Pickering emulsions

## Slide 20
Q-4
Porod law :
Smooth interface
Deviation from Porod law :
Rough Interface
NCC do not dive into oil
Adsorbed via an hydrophobic facet ?
F. Cherhal et al, Biomacromolecules, 2016, 17(2), pp 496–502
Pickering emulsions

## Slide 21
Outline…
Pickering emulsions based on cellulose nanocrystals
Foams and Neutron Scattering
Strategy 2 : Smart Foams based on fatty acids
Ultrastable and thermo-stimulable foams
Strategy 1 : Foams based on SDS and salt
Ultrastable and thermo-stimulable foams

## Slide 22
air
liquid
air
air
Thin film
Plateau border
bubble
Foams and Neutron Scattering
What is a foam ?

## Slide 23
Foams and Neutron Scattering
Discussion on scattering events (reflectivity versus SANS)
Film thickness in dry foams
Bulk structure in Plateau border in wet foams
Contrast matching strategies
Kinetics of drainage ( from incoherent scattering)

## Slide 24
Thin film
Interface
Volume
Foams and Neutron Scattering
Contrasts in foams

## Slide 25
rhydrogenated surfactants ~ 0 close to rH2O
Volume
Foams and Neutron Scattering
Contrasts in foams

## Slide 26
rhydrogenated surfactants ~ 0 = rair = r92%H2O/8%D2O
Volume
Foams and Neutron Scattering
Contrasts in foams
Matching is possible !

## Slide 27
Volume
Thin film
Interface
rhydrogenated surfactants ~ 0 very different from rD2O
Good contrast for measurements
Foams and Neutron Scattering
Contrasts in foams

## Slide 28
Volume
Thin film
Interface
Dry foams : scattering from thin films is dominant
Foams and Neutron Scattering
Contrasts in foams

## Slide 29
Volume
Thin film
Interface
Wet foams : scattering from Plateau border is dominant
Foams and Neutron Scattering
Contrasts in foams

## Slide 30
Foams and Neutron Scattering
Scattering in dry foams
Reflectivity from the different thin films
« Spikes » on the 2D-detector
(First article using SANS and foams)
M. Axelos, F. Boué, Langmuir, 2003,19(17), 6598–604

## Slide 31
Foams and Neutron Scattering
Scattering in dry foams
« Spikes » on the 2D-detector
(First article using SANS and foams)
Measurement of the reflectivity curve of the thin film
Determination of the thickness of the film via Kiessieg finges
Isotropic averaging : signal of powder of thin films
Micheau C, Bauduin P, Diat O, Faure S., Langmuir, 2013, 29(27), 8472–81
M. Axelos, F. Boué, Langmuir, 2003,19(17), 6598–604

## Slide 32
Foams and Neutron Scattering
Scattering in wet foams made from mixtures
Volume
Interface

## Slide 33
Contrast variation enables to probe selectively interface or Plateau border
Volume
Interface
Foams and Neutron Scattering
Scattering in wet foams made from mixtures

## Slide 34
Foams and Neutron Scattering
Example : mixture of silica nanoparticles and SDS
Scattering in wet foams made from mixtures

## Slide 35
Foams and Neutron Scattering
Scattering in wet foams made from mixtures
Determination of the composition of the silica nanoparticles/SDS foam ?

## Slide 36
Foams and Neutron Scattering
Scattering in wet foams made from mixtures
Determination of the composition of the silica nanoparticles/SDS foam ?
Consider both coherent and incoherent scattering
Coherent scattering
« 2 components » system :
Nanoparticles versus water and air
Incoherent scattering
« 2 components » system :
Water versus air and nanoparticles (sinc(SiO2) = 0)

## Slide 37
Foams and Neutron Scattering
Scattering in wet foams made from mixtures
Determination of the composition of the silica nanoparticles/SDS foam ?
Consider both coherent and incoherent scattering
Coherent scattering
« 2 components » system :
Nanoparticles versus water and air
Incoherent scattering
« 2 components » system :
Water versus air and nanoparticles (sinc(SiO2) = 0)

## Slide 38
Foams and Neutron Scattering
Scattering in wet foams made from mixtures
Its is possible to follow the reorganizations within Plateau during drainage process !
Determination of the composition of the silica nanoparticles/SDS foam ?

## Slide 39
Outline…
Pickering emulsions based on cellulose nanocrystals
Foams and Neutron Scattering
Strategy 2 : Smart Foams based on fatty acids
Ultrastable and thermo-stimulable foams
Strategy 1 : Foams based on SDS and salt
Ultrastable and thermo-stimulable foams

## Slide 40
Ultrastable and thermostimulable foams
How to make a foam with a long lifetime, based on usual and cheap compounds, whom stability can be tuned by an external stimuli ?

## Slide 41
Drainage
Coarsening
Coalescence
gaz
g
Why is a foam not stable ?
Ultrastable and thermostimulable foams

## Slide 42
air
air
air
Make an elastic film to limit coalescence and coarsening
Slowing the drainage by increasing the viscosity in the Plateau borders
Ultrastable and thermostimulable foams
How to design a stable foam ?

## Slide 43
air
air
air
Use of nanoparticles (« Pickering » foams)
Ultrastable and thermostimulable foams
How to design a stable foam ?

## Slide 44
air
air
air
• Only a few amount of foam is made (stabilizers do not go fast up to interfaces when gaz is incoporated)
• It is difficult to tune the stability of foam by an external stimulus
But…
Ultrastable and thermostimulable foams
How to design a stable foam ?
Use of nanoparticles (« Pickering » foams)

## Slide 45
Surfactants
Nanoparticles
Good foamability
Good stability
Ultrastable and thermostimulable foams
How to obtain both a good foamability and a good stability ?

## Slide 46
Ultrastable and thermostimulable foams
How to obtain both a good foamability and a good stability ?
Dodécylsulfate de sodium (SDS)
Use a very common surfactant (SDS)
…. and salt !
+
Strategy 1
Use self-assembly of fatty acids
Strategy 2
2 amino 1 ethanol

## Slide 47
Ultrastable and thermostimulable foams
How to obtain both a good foamability and a good stability ?
Dodécylsulfate de sodium (SDS)
Use a very common surfactant (SDS)
…. and salt !
+
Strategy 1
Use self-assembly of fatty acids
Strategy 2
2 amino 1 ethanol

## Slide 48
-
-
-
-
-
-
-
-
-
+
+
+
+
+
+
Na+
-
Cl-
Strategy 1 Foams based on SDS and salt
Water + 69 mM SDS
Stability ~ few hours

## Slide 49
-
-
-
-
-
-
-
-
-
+
+
+
+
+
+
+
Na+
-
Cl-
-
-
-
+
+
+ 250 mM of NaCl
Stability decreases
(electrostatic screening)
Water + 69 mM SDS
Stability ~ few hours
Strategy 1 Foams based on SDS and salt

## Slide 50
-
-
-
-
-
-
-
-
-
+
+
+
+
+
+
+
Na+
Water + 69 mM SDS
Stability ~ few hours
-
Cl-
-
-
-
+
+
+ 500 mM of NaCl
Stability increases back!!!
+
-
+
-
Strategy 1 Foams based on SDS and salt

## Slide 51
-
-
-
-
-
-
-
-
-
+
+
+
+
+
+
Na+
-
Cl-
What about KCl ?
+
K+
Water + 69 mM SDS
Stability ~ few hours
Strategy 1 Foams based on SDS and salt

## Slide 52
-
-
-
-
-
-
-
-
-
+
+
+
+
+
Na+
-
Cl-
-
-
-
+
Ultrastables foams…
+
K+
+
+
+
+ 500 mM of NaCl
+ 250 mM of KCl
Water + 69 mM SDS
Stability ~ few hours
Strategy 1 Foams based on SDS and salt

## Slide 53
-
-
-
-
-
-
-
-
-
+
+
+
+
+
Na+
-
Cl-
-
-
-
+
… over several months!
+
K+
+
+
+
Strategy 1 Foams based on SDS and salt
+ 500 mM of NaCl
+ 250 mM of KCl

## Slide 54
NaCl
KCl
Scattering by the interfaces of bubbles
(Porod law)
Neutrons
(SANS)
Origin of stability ?
Strategy 1 Foams based on SDS and salt

## Slide 55
Neutrons
(SANS)
NaCl
KCl
Presence of crystals of lamellar phases within foams !
Origin of stability ?
Strategy 1 Foams based on SDS and salt

## Slide 56
Optical microscopy
Optical microscopy
Non spherical droplets :
Solid-like Interfaces
Adsorption of crystals at interfaces
Presence of crystals in solution
Origin of stability ?
Strategy 1 Foams based on SDS and salt

## Slide 57
The formation of crystals enable to limit the 3 mechanims of destabilization of foams
Strategy 1 Foams based on SDS and salt
Origin of stability ?

## Slide 58
Origin of differences between Na+ and K+ ?
Strategy 1 Foams based on SDS and salt
+ 500 mM of NaCl
+ 500 mM of KCl
???

## Slide 59
+ 500 mM of NaCl
+ 500 mM of KCl
???
Origin of differences between Na+ and K+ ?
Strategy 1 Foams based on SDS and salt
Influence of kinetics of formation of crystals
Time of apparition of crystals by eye after cooling from an homogeneous phase
Crystals are made much faster with KCl than with NaCl

## Slide 60
+ 500 mM of NaCl
+ 500 mM of KCl
???
Origin of differences between Na+ and K+ ?
Strategy 1 Foams based on SDS and salt
Influence of kinetics of formation of crystals
Crystals are made much faster with KCl than with NaCl
Competition between the kinetics of formation of crystals and kinetics of destabilization of foams

## Slide 61
Surfactants concentration
Temperature
Tk
CMC
monomers
micelles
Phase diagram of surfactants
Heat the sample above the Krafft temperature Tk !!
How to destabilize above a given temperature ?
Strategy 1 Foams based on SDS and salt

## Slide 62
Optical microscopy
Heating above Tk
Strategy 1 Foams based on SDS and salt
How to destabilize above a given temperature ?

## Slide 63
Outline…
Pickering emulsions based on cellulose nanocrystals
Foams and Neutron Scattering
Strategy 2 : Smart Foams based on fatty acids
Ultrastable and thermo-stimulable foams
Strategy 1 : Foams based on SDS and salt
Ultrastable and thermo-stimulable foams

## Slide 64
A.-L. Fameau et al, Angewandte Chemie Int. Ed., 2011, 50, 8264 –8269.
12 hydroxy-staric acid
New green surfactants
Strategy 2 Smart Foams based on fatty acids
Outstanding stability at ambient temperature!
2 amino 1 ethanol

## Slide 65
A.-L. Fameau et al, Angewandte Chemie Int. Ed., 2011, 50, 8264 –8269.
12 hydroxy-staric acid
New green surfactants
°
°
°
Outstanding stability at ambient temperature!
First thermoresponsive foams described in literature
2 amino 1 ethanol
Strategy 2 Smart Foams based on fatty acids

## Slide 66
20°C
47°C
50°C
60°C
10µm
A.-L. Fameau, F. Cousin, L. Navailles, F. Nallet, F. Boué, J.-P. Douliez, J. Phys. Chem. B, 2011, 115(29), 9033–9039.
Behavior in bulk Smart Foams based on fatty acids

## Slide 67
20°C
47°C
50°C
60°C
10µm
A.-L. Fameau, F. Cousin, L. Navailles, F. Nallet, F. Boué, J.-P. Douliez, J. Phys. Chem. B, 2011, 115(29), 9033–9039.
2 amino 1 ethanol
Multilamellar tubes
Behavior in bulk Smart Foams based on fatty acids

## Slide 68
20°C
47°C
50°C
60°C
10µm
A.-L. Fameau, F. Cousin, L. Navailles, F. Nallet, F. Boué, J.-P. Douliez, J. Phys. Chem. B, 2011, 115(29), 9033–9039.
2 amino 1 ethanol
Multilamellar tubes
Behavior in bulk Smart Foams based on fatty acids

## Slide 69
20°C
47°C
50°C
60°C
70°C
10µm
?
70°C
A.-L. Fameau, F. Cousin, L. Navailles, F. Nallet, F. Boué, J.-P. Douliez, J. Phys. Chem. B, 2011, 115(29), 9033–9039.
Behavior in bulk Smart Foams based on fatty acids

## Slide 70
20°C
47°C
50°C
60°C
70°C
10µm
?
A.-L. Fameau, F. Cousin, L. Navailles, F. Nallet, F. Boué, J.-P. Douliez, J. Phys. Chem. B, 2011, 115(29), 9033–9039.
Melting of tubes into micelles at high T!
Behavior in bulk Smart Foams based on fatty acids

## Slide 71
D2O
air
D2O
≈300 Å
2π/∆Q
air
air
D2O
21 Å
Experimental data
Behavior at air/water interface Smart Foams based on fatty acids

## Slide 72
80%D2O/20%H2O
100%D2O
60%D2O/40%H2O
R
Neutron Reflectivity or SANS ?
Behavior at air/water interface Smart Foams based on fatty acids

## Slide 73
80%D2O/20%H2O
100%D2O
60%D2O/40%H2O
RQ4
Neutron Reflectivity or SANS ?
Behavior at air/water interface Smart Foams based on fatty acids

## Slide 74
z
d
Ffatty acids (z)
Experimental data
Model of adsorbed tubes
Adsorption of the tubes at the air/water interface!
Behavior at air/water interface Smart Foams based on fatty acids

## Slide 75
Structure at the interface tuneable with temperature!
20°C
50°C
60°C
70°C
A.-L.Fameau, J-P. Douliez, F. Boué, F.Ott, F. Cousin, J. Colloid Interface Sci., 2011, 362, 397-405
Behavior at air/water interface Smart Foams based on fatty acids

## Slide 76
Drained liquid
foam
Initial stock solution
Tubes have the same structure in bulk solution and whithin the foam
Smart Foams

## Slide 77
film
interface
Ultrastable foams
air
air
air
Plateau borders
At 20°C
Limitation of the drainage!
Smart Foams

## Slide 78
t=0 min
t=3 min
t=6 min
t=9 min
t=15 min
Evolution at 70°C
Fast destabilization!
Smart Foams

## Slide 79
T=3 min at 70°C
t=3 min
+
Melting of the tubes into micelles
Smart Foams

## Slide 80
T=5 min at 70°C
t=6 min
Stock solution : micelles
Foam
Formation of micelles in situ within the foam
Smart Foams

## Slide 81
film
air
air
air
Plateau borders
interface
Unstable foams
At 70°C
Fast destabilization due to tubes/micelles transition!
Smart Foams

## Slide 82
Foam
?
?
?
solution
Air/water interface
?
NR/SANS Smart Foams

## Slide 83
Thanks to…
Isabelle Capron(BIA Nantes, Fanch Cherhal (BIA Nantes)
Anne-Laure Fameau(LLB, BIA Nantes), Jean-Paul Douliez (BIA Nantes), Arnaud Saint-Jalmes (IPR Rennes), François Boué (LLB)
Anniina Salonen, Alesya Mikhailovskaya, Li Zhang, Pavel Yasghur, Dominique Langevin (LPS Orsay), François Muller (ECE paris/LLB), François Boué (LLB)